**Epoxy phosphate**

801

Features and advantages:

1, is a kind of epoxy modified phosphate ester multifunctional group paint dense agent, can improve the coating on the metal surface of the dense To improve the ductility and impact resistance of the film;

2, the adhesion group interacts with the metal surface, and the adhesion promoter is well oriented in the substrate, so as to improve Adhesion. It can obviously improve the adhesion to metal substrate, film flexibility, water resistance, cup convex and fog resistance Performance.

3. Adhesion promoter contains a large number of substrate reaction groups, which can be easily carried out with hydroxyl groups in the substrate system Cross linking reaction. Suitable for coil steel coating, can coating, anti-theft door, car coating, etc., can be sprayed, dip coating And the spray coating. Suitable for polyurethane system, acrylic system and epoxy phenolic system.

4, does not affect the storage and coating film weather resistance; Can withstand high temperature baking above 200℃, high temperature rapid Bake does not change color;

**Product specifications:**

|  |  |
| --- | --- |
| appearance | Light yellow transparent liquid |
| Valid copy of | 90% |
| composition | Epoxy modified phosphate ester |

**Application areas:**

Tinplate, coil steel, cast iron, aluminum material alloy, electroplating surface, aluminum magnesium alloy, plastic and other surfaces Richard.

**Recommended dosage:** 0.5-2% of total formula (please test the most appropriate dosage before use)

**Usage:** Add before and after grinding.

**Packaging:** 25kg/200kg non-recycled plastic drum. The product is not completely used, the lid must be tightly closed after use.

**Storage:** keep away from heat and fire and keep away from light.